# How to torch braze aluminum

## Helpful Video

This video will explain everything you need to know, but if you’re too lazy to watch it, you can read the directions below.

## Materials

You can get all of these materials at Home Depot or Amazon:

- Propane Torch

- Torch Trigger

- Aluminum brazing and welding rods

- Aluminum Tubing

## Steps

*Note: When brazing, the filler rod will always flow towards the heat. Had you clamped your setup vertically and gotten the joint a fair bit hotter, you could have drawn the molten filler towards the torch. could make for a significantly stronger joint.

*Note: For better results, work on a ceramic topped table with a ceramic tile behind the metal you're working on. Try to place ceramic on the sides also. This will reflect a good portion of heat which will otherwise dissipate very quickly.

- Chamfer the ends of the aluminum where you are going to bond it (to allow a channel for the braising material)

- Clean the aluminum with a brush

- Clamp up the tubing

- Start heating the intended area with the propane torch (get it to around 700 degrees)

  - This may take 4-5 minutes

  - We want it hot enough to melt the brazing rod but not the aluminum

- When you think you’ve reached that point start moving the rod down the chamfered channel and when it starts to melt you are hot enough

- Rub the brazing rod until its filled in then finish off with some heat

- Repeat process on all sides of the aluminum joint

## Additional resources

Working with braze aluminum

Wiki-How